# Technical Data Sheet

Pileman®

| Parameter | unit | Results |
| --- | --- | --- |
| Free Swelling Volume | ml | 28-33 |
| pH (3% dispersion) | - | 8.5 - 9.5 |
| Moisture | % | 12 max |
| Loose Bulk density | g/cm3 | 0.85 ±10% |
| Dry residue # 200 | % | 15max |
| Wet residue # 200 | % | <2% |

| Rheology in fresh water - No ageing time |
| --- |
| Concentration | Kg/m3 | 50 |
| Marsh Viscosity | Sec/qt | 40 |
| Gel Strength | Pa | 7 |
| Yield | bbl/sht | 110 |
| API filtrate (30 min under7kg/cm2) | ml | 20 -22 |

Table 1

| Pileman® Concentration @ 50kg in 1000 ltr fresh water | Easy-Bore polymer Powder | Easy-Bore Polymer Gel | Am-PAC | Fann VDR 600 RPM | Gel strength Pa | Fluid Loss 22.5 Min. On 50kg/m3 concentration |
| --- | --- | --- | --- | --- | --- | --- |
| Pileman® | …… | 500 gm | …… | 40 | 10” Gel=10 10’ Gel=11.5 | 19.5 ml |
| Pileman® | …… | 750 gm | 50 gm | 44 | 10” Gel=12 10’ Gel=13.5 | 18 ml |
| Pileman® | 150 gm | …… | …… | 52 | 10” Gel=13 10’ Gel=14.5 | 18.5 ml |
| Pileman® | 150 gm | …… | 50 gm | 46 | 10” Gel=13 10’ Gel=14.5 | 17.5 ml |

| For low Speed Mixing (results based on 1500 RPM mixer for 3 Min) and after 1-hour standby time | Easy-Bore Polymer Powder | Easy-Bore Polymer Gel | Am-PAC | Instant Marsh Viscosity. (Sec/Qt) | One Hr. Stand by Marsh Viscosity. (Sec/Qt) | Fluid Loss 22.5 min. (ml) |
| --- | --- | --- | --- | --- | --- | --- |
| Pileman® 50kg in 1m3 Fresh water | …… | 500 gm | …… | 43 | 47 | 20 |
| Pileman® 50kg in 1m3 Fresh water | …… | 750 gm | 50 gm | 44 | 48 | 18.5 |
| Pileman® 50kg in 1m3 Fresh Water | 150gm | …… | 50 gm | 48 | 51 | 18 |
| Pileman® 50kg in 1m3 Fresh Water | 150gm | …… | …… | 52 | 57 | 19.5 |

Table 2

[Star Export House accreditation by Govt. of India ]

ISO 9001 : 2015  Quality System

# Text boxes

# Mixing procedure:

Simply mix 50 kg of Pileman® in 1000 ltr. fresh water and the slurry will be ready to use within 20 minutes of mixing, giving a marsh viscosity of 40”

The water for slurry making should be treated with soda ash – light for any carbonate hardness. In case of high chloride content please refer to us for technical assistance

General Description:

Pileman® is high yield sodium activated bentonite made from extrusion process.

It is superbly adaptable to requirement of all vertical drilling like bore Piling, D-walling and similar technologies.

This product has been in the market for more than 10 years and has proven well. Its unique formula is able to hold the wall of the pile and the collapse is minimal.

It does not contain any polymer but is designed to work alongwith. Hence if you encounter different soil condition there will be no need to change to a different bentonite, just add our polymer/additives to get the required slurry properties.

# Product features:

- Yield of 110 bbl./sht

- Produces thixotropic Gel

- The slurry is designed to deposit thin

impermeable filter cake, ensuring low

fluid loss.

- Cools as well as lubricates drilling bit.

- Low sand content, protects your expensive

mud pump liners.

- Properly calibrated to work with Easy-Bore™

(Polymer Gel) & AmPAC™ (Cellulose)

Pileman® has good compatibility with organic

additives like Polymer and Cellulose. The chart on

table 1 is the guide for Rheology. With change in soil

profile say normal to sandy, gravel or rock the use

of polymers is recommended.

In case high speed mixer is not available on

Site, Pileman can still deliver same Rheology

on slow mixing process with just one hour

ageing time. Please refer to table 2 in the

following page.

Corporate  & Marketing Office :

32A,Chittaranjan Avenue, Calcutta 700012, India

Ph:   +91 33 4007 2855  |  Mobile: +91 9831013136

Fax:  +91 33 2212 2040

Email:  amrfeo@amrfeo.com  or  amrfeo@gmail.com

Web   : www.amrfeo.com

Bentonite Processing plant :

Survey no: 583/1 plot 2-6, Bhuj Bacaho Road

Kutch – Gujarat , India

Only in-house production & process:

Bentonite | Drilling Polymer & Cellulose | Drilling Foam | Bentonite Pellets| Super Absorbent Clay